(Note to Specifier:  This specification has additional instructions included as Hidden Text.  To view this information, Select Tools, Options, and check Hidden Text in the Formatting Marks section of the View Tab.)

2004 MASTER FORMAT™ SECTION 06 06 60

Schedules for Plastic Fabrications

3form Translucent Resin Panel System

GENERAL

RELATED DOCUMENTS

Drawings and general provisions of the Contract, including General and Supplementary Conditions and other Division 1 Specification sections, apply to this Section.

summary

This Section includes the Plastic Fabrication as shown and specified in the described system(s):

Adjust list below to suit Project

Appliqués

Backsplashes

Balustrade Panels

Bar fronts

Bus Shelters

Cabinet Doors

Light-Diffusing Ceiling Panels

Closet Doors

Door Lights

Doors

Flooring

Lighting

Projection screens

Retail Shelving

Sculpture

Shower doors & enclosures

Side lights

Signage

Tabletops

Transaction Tops

Vanity tops

Wall Sculpture

Water walls

Whiteboards

Worktops

[Insert Item]

The extent of Solid Polymer Fabrication is shown on the drawings.

Additional fabrication and installation details from 3form technical department, if applicable

Related Sections include the following:

Adjust list below to suit Project

Section 05 73 00 Decorative Metal Railings

Section 06 06 20 Schedules for Finish Carpentry; Section 06 06 40 Schedules for Architectural Woodwork; Section 06 06 50 Schedules for Structural Plastics; Section 06 06 60 Schedules for Plastic Fabrications; Section 06 06 70 Schedules for Structural Composites; Section 06 06 80 Schedules for Composite Assemblies

Section 08 15 00 Plastic Doors; Section 08 80 00 Glazing

Section 10 11 00 Visual Display Surfaces; Section 10 14 00 Signage; Section 10 21 00 Compartments and Cubicles; Section 10 22 00 Partitions;

Section 12 36 23 Plastic Countertops

Administrative requirements

Project Pre-installation Meeting

Owner, Architect, Contractor, Installer to meet at project site within one week of scheduled installation.

Review mounting conditions, installation and storage instructions, fabrication requirements, seaming and protection measures.

submittals

General:  Submit the following in accordance with conditions of contact and Division 1 specification section 01 33 00 “Submittal Procedures”.

Product List: Minimum of 3 completed 3form Chroma installations or 3 installations of similar materials and complexity. Include contact name and email address for each product.

Product Data:  Submit manufacturer’s product data; include product description, fabrication information, and compliance with specified performance requirements.

Submit product test reports from a qualified independent 3rd party testing agency indicating each type and class of panel system complies with the project performance requirements, based on comprehensive testing of current products.  Previously completed test reports will be acceptable if for current manufacturer and indicative of products used on this project.

Test reports required are:

Rate of Burning (ASTM D 635)

Self-Ignition Temperature (ASTM D 1929)

Density of Smoke (ASTM D 2843)

Steiner Tunnel (ASTM E84)

Dynamic environmental testing (ASTM standards D 5116 or D 6670)

Coefficient of Friction (ASTM 2047)

Building Approvals: Plastic Fabrications are to have been evaluated and must be registered with and comply to requirements of the following jurisdictions:

Los Angeles Department of Building and Safety (Product must have a LARR [Los Angeles Research Report] number) for use as Light-transmitting Panels

ICC-ES Report for Light Transmitting Plastics and Interior Finishes

Shop Drawings:  Include plans, elevations, sections, panel dimensions, details, and attachments to other work.

Samples for Initial Selection:

Submit minimum 2-inch by 2-inch samples.  Indicate full color, texture and pattern variation.

Samples for Verification:

Submit minimum 4-inch by 4-inch sample for each type, texture, pattern and color of solid plastic fabrication.

Delete below if mockups are not required

Mockups:

Build mockups to verify selections made under sample Submittals and to demonstrate aesthetic effects.

Build mockup of [each type of] Plastic Fabrication.

Retain subparagraph below if mockups are erected as part of building rather than separately

Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Maintenance Data:  Submit manufacturer’s care and maintenance data, including care, repair and cleaning instructions.  Include in Project closeout documents.

quality assurance

Manufacturers Qualifications

Materials and systems shall be manufactured by a company continuously and regularly employed in the manufacture of specified materials for a period of at least three (3) consecutive years and which can show evidence of those materials being satisfactorily used on at least three (3) projects of similar size, scope and location. At least one (1) of the projects shall have been successful for use one year or longer.

Manufactured panels must be produced from a minimum of 38% pre-consumer recycle content and 9% post-consumer recycled content or a minimum total recycled content factor of 0.20.  This recycle content must be certified by a recognized 3rd party certification group, such as Scientific Certification Systems (SCS).

Completely PVC – Free product

Manufacturer must offer a documented reclaim process that will take back, at the manufacturers cost, panels that are at their end-of life cycle.  Return process is preceded by following requirements highlighted in Section 02 42 00 Removal and Salvage of Construction Materials.

Manufacturer must have a 3rd party completed Life Cycle Analysis

Manufacturer must have an Environmental Product Declaration (EPD).

delivery, storage, and handling

Deliver Plastic Fabrications, systems and specified items in manufacturer’s standard protective packaging.

Do not deliver Plastic Fabrications, system, components and accessories to Project site until areas are ready for installation.

Store materials in a flat orientation in a dry place that is not exposed to exterior elements. Materials are to be protected against damage from moisture and direct sunlight.

Store 3form Chroma in area of installation minimum of 24 hours prior to installation.

Handle materials to prevent damage to finished surfaces.  Provide protective coverings to prevent damage or staining following installation for duration of project.

Before installing Plastic Fabrications, permit them to reach room temperature.

Project Conditions

Environmental Limitations:  Do not install Solid Polymer Fabrications until spaces are enclosed and weatherproof, and ambient temperatures and humidity conditions are maintained at the levels indicated for Project when occupied for its intended use.

Warranty

Manufacturer’s Special Warranty on Plastic Fabrications:  Manufacturer’s standard form agreeing to repair or replace units that fail in material or workmanship within the specified warranty period.

Warranty Period:  1 year after ship date.

PRODUCTS

Manufacturer

Manufacturer:  3form, LLC., Salt Lake City, Utah, USA / telephone 801-649-2500

Materials

3form Chroma

Engineered acrylic resin produced in the USA

Sheet Size: Maximum 4’ x 10’

Thickness: Minimum 1/2”

Basis of Design Product:  The design of Plastic Fabrications is based on Chroma as provided by 3form, Inc. Products from other manufacturers must be approved by the Architect or Designer prior to bidding in accordance with the Instructions to Bidders and Section 10 60 00 “Product Requirements”.  3form designs are protected by registered copyrights and patents, and may not be duplicated. Copied designs will be considered a violation of intellectual property rights and will be pursued.

Sheet minimum performance attributes:

Rate of Burning (ASTM D 635).  Material must attain CC2 Rating for a nominal thickness of 1.5 mm (0.060 in.) and greater.

Self-Ignition Temperature (ASTM D 1929).  Material must have a Self-ignition temperature greater than 850°F.

Density of Smoke (ASTM D 2843).  Material must have a smoke density less than 10%.

Coefficient of Friction (ASTM 2047) 0.73 Dry, 0.79 Wet

Dynamic environmental testing (ASTM standards D 5116 or D 6670).  Panels must not have detectable VOC off-gassing agents and must be have Greenguard™ Indoor Air Quality Children and Schools certified.

Product must be fused using heat and pressure, not laminated with adhesives.

Color must be PVC-Free and be an acrylic resin made with pigments, not dyes. Must be UV stable colors

Vellum surface should be completely renewable onsite.

fabrication

General:  Fabricate Plastic Fabrications to designs, sizes and thicknesses indicated and to comply with indicated standards.  Sizes, profiles and other characteristics are indicated on the drawings, additional fabrication and installation details can be found on the 3form Fabrication Drawings.

Comply with manufacturer’s written recommendations for fabrication.

Machining:  Acceptable means of machining are listed below. Ensure that material is not chipped or warped by machining operations.

Sawing: Select equipment and blades suitable for type of cut required.

Drilling: Drills compatible with plastic products.

Routing

Laser Cutting

Laser Etching

Forming:  Form products to shapes indicated using the appropriate method listed below.  Comply with manufacturer’s written instructions.

Cold Bending

Hot Bending

Thermoforming: Acceptable only on uncoated material.

Drape Forming

Matched Mold Forming

Mechanical Forming

Laminating:  Laminate to substrates indicated using adhesives and techniques recommended by manufacturer.

Bonding

Manufacturer must have an in-field seaming process and fabrication kit including necessary adhesive and tools.

Miscellaneous Materials

General: Provide products of material, size, and shape required for application indicated, and with a proven record of compatibility with surfaces contacted in installation.

Cleaner:  Type recommended by manufacturer.

Adhesives: May be achieved with 2-part adhesives or silicones, suitable for use with product and application.

EXECUTION

examination

Examine substrates, areas, and conditions where installation of Plastic Fabrications will occur, with Installer present, for compliance with manufacturer’s requirements.  Verify that substrates and conditions are satisfactory for installation and comply with requirements specified.

installation

General:  Comply with manufacturer’s written instructions for the installation of Plastic Fabrications. Sizes, profiles and other characteristics are indicated on the drawings, additional installation details can be found on the 3form Certified Installer, if applicable.

Manufacturer’s shop to fabricate items to the greatest degree possible.

Utilize fasteners, adhesives and bonding agents recommended by manufacturer for type of installation indicated.  Material that is chipped, warped, hazed or discolored as a result of installation or fabrication methods will be rejected.

Install components plumb, level and rigid, scribed to adjacent finishes, in accordance with approved shop drawings and product data.

Form field joints using manufacturer’s recommended procedures.  Locate seams in panels so that they are not directly in line with seams in substrates.

We recommend that installation is completed by a 3form Certified Installer. Contact 3form for more information or to get a quote.

cleaning and protection

Protect surfaces from damage until date of substantial completion.  Repair work or replace damaged work, which cannot be repaired to Architect’s satisfaction.

End of Section 06 06 60

Solid Polymer Fabrication #1 (SPF-1)

Product:	[Replace with Collection and product name]

Color:	[Replace with color name]

Gauge:	[1/2"][1"][2”][As indicated on drawings][As required to meet deflection requirements]

Surface Finish:	[Vellum][Stucco][Velvet][Grain][Grid]Patent][Sandstone][Patina]

UV Protection is desirable for applications that will receive direct sunlight.

UV Protection: 	[required][not required]

Refer to www.3-form.com for expansion/contraction information.  This information is required for applications subjected to temperature variation.

Expansion/Contraction Allowance:

Orientation: 	[Horizontal][Vertical]

Repeat Product Data Sheets as required to identify all Varia™ applications.